Contents lists available at ScienceDirect

Environmental Research

journal homepage: www.elsevier.com/locate/envres

Environmental Research 193 (2021) 110587

Facile hydrothermal synthesis of rod-like Nb2O5/Nb2CTx composites for	 visible-light driven photocatalytic degradation of organic pollutants

Ce Cui a, Ronghui Guo a,*, Erhui Ren a, Hongyan Xiao a, Xiaoxu Lai a, Qin Qin a,

Shouxiang Jiang b, Hong Shen a, Mi Zhou a, Wenfeng Qin c

a College of Biomass Science and Engineering, Sichuan University, Chengdu, 610065, China

b Institute of Textiles and Clothing, The Hong Kong Polytechnic University, Kowloon, Hong Kong, China

c Aviation Engineering Institute, Civil Aviation Flight University of China, Guanghan, China

A R T I C L E I N F O

Keywords:

Nb2CTx

Rod-like Nb2O5/Nb2CTx Hydrothermal oxidation Photocatalytic degradation Organic pollutants

A B S T R A C T

The MXene-based transition metal oxide composite is a potential candidate for photocatalysts. Rod-like pseu- dohexagonal phase Nb2O5/Nb2CTx composites were synthesized by a simple hydrothermal oxidation of 2D layered Nb2CTx. The Nb2O5/Nb2CTx composites show superior photocatalytic activity for 98.5% of degradation of Rhodamine B (RhB) for 120 min and 91.2% of tetracycline hydrochloride (TC-HCl) for 180 min under visible light irradiation. The Schottky junction is formed between Nb2O5 nanorods and Nb2CTx and the photo-generated carriers are effectively separated, enhancing the photocatalytic activity of the Nb2O5/Nb2CTx. High photoactivity and cycle stability of Nb2O5/Nb2CTx composites indicate that hydrothermal oxidation of 2D layered Nb2CTx is an alternative to prepare efficient photocatalyst for degradation of organic pollutants.

# Introduction

In recent years, worldwide water pollution caused by discharge or improper handling of organic pollutants such as dyes and antibiotics has become a huge challenge to ecosystem and human life (Adhikari et al., 2019; Di et al., 2015; Lin et al., 2017b; Rimoldi et al., 2017). The pho- tocatalysts with high specific surface area and excellent photoactivity are highly efficient materials to removing contaminants from water. Nb2O5, as a typical transition metal oxide semiconductor photocatalyst exhibits good chemical stability, nontoxicity and commercial avail- ability (Chen et al., 2017; Hong et al., 2016; Li et al., 2013; Oliveira et al., 2014; Zhang et al., 2018). Nevertheless, Nb2O5 suffers charge recombination of photogenerated electrons and holes, resulting in

MXenes, as a new family of 2D materials, exhibit excellent structural stability, electrical conductivity and surface hydrophilicity (Ding et al., 2017; Ran et al., 2017; Wang et al., 2018; Zhao et al., 2019). MXene have been served as cocatalysts for photocatalysts to accelerate the separation of charge carriers (Liu et al., 2018; Wang et al., 2016). Recently, the heterogeneous compounds composed of MXene and cor- responding oxides have been used in the field of photocatalysis (Peng et al., 2017; Shahzad et al., 2018). A hybrid composed of (001) TiO2 nanosheets and layered Ti3C2 MXene exhibits enhanced photocatalytic degradation of dyes (Peng et al., 2016). Nb2CTx MXene has been used as a promising co-catalyst for photocatalytic hydrogen evolution of TiO2. Nb2CTx was more beneficial to improve photocatalytic activity of TiO2 than Ti3C2Tx (Wang et al., 2016). Recently, Nb2O5/C/Nb2C hybrid

limited photocatalytic efficiency (Wang et al., 2019). Therefore, con-

material was synthesized by one-step CO2 oxidation technique of

struction of heterojunctions is an effective method to enhance the photoactivity of Nb2O5. Currently, some heterojunctions such as g-C3N4/Nb2O5, TiO2/Nb2O5 and rGO/Nb2O5 have been used in photo- oxidation of pollutants and photocatalytic hydrogen generation (da Silva et al., 2017; Li et al., 2019a; Li et al., 2019b; Ren et al., 2019; Yi et al., 2019). However, molecular-scale interfacial heterojunction causes defect-induced recombination of photogenerated carriers, which affects photocatalytic performance.

Nb2CTx for hydrogen production (Su et al., 2018). However, the morphology of Nb2O5 cannot be effectively controlled to further improve the photocatalytic activity of the composite. Generally, the activity of Nb2O5 can be significantly affected by its shape and surface structure (Du et al., 2018; Wang et al., 2019). Nb2O5 with nanowires, nanospheres, nanorods and other special shape can increase their spe- cific surface area, thereby enhancing photocatalytic performance (Jiang et al., 2018; Li et al., 2013; Qamar et al., 2015; Zhang et al., 2018; Zhao

* Corresponding author.

E-mail address: ronghuiguo214@126.com (R. Guo).

https://doi.org/10.1016/j.envres.2020.110587

Received 17 February 2020; Received in revised form 30 October 2020; Accepted 2 December 2020

Available online 9 December 2020

0013-9351/© 2020 Elsevier Inc. All rights reserved.

et al., 2012). Although the composites of Nb2O5 and Nb2CTx were fabricated for charge storage and hydrogen production (Liu et al., 2018; Zhang et al., 2016a), however, the complex of Nb2O5 and Nb2CTx with special morphology for photocatalytic degradation of organic pollutants have not been reported.

In this study, the layered Nb2CTx was used to fabricate rod-like Nb2O5/layered Nb2CTx (Nb2O5/Nb2CTx) composite through a facile hydrothermal oxidation with no additional Nb source (Fig. 1). The Nb2O5 nanorods were grown on the surface of Nb2CTx during hydro- thermal oxidation of Nb2CTx. The visible-light photocatalytic activity of Nb2O5/Nb2CTx composites was evaluated by decomposition of the representative rhodamine B (RhB) and tetracycline hydrochloride (TC- HCl).

# Experimental

  - Materials and reagents

≥

Hydrofluoric acid (HF, content 40.0%), rhodamine B (RhB) and tetracycline hydrochloride (TC-HCl) were provided by Chengdu Kelong chemical reagent factory Co., Ltd., China. Nb2AlC (200 M) was pur- chased from Forsman Scientific (Beijing) Co., Ltd.

  - Synthesis of layered Nb2CTx

≥

In order to synthesize layered Nb2CTx, 1 g Nb2AlC was placed into 60 mL HF solution (content 40.0%) and stirred at 55 ◦C for 90 h. The resulting suspension was centrifuged with deionized water for several times until pH ≥ 6. The layered Nb2CTx sediment was then dried.

  - Synthesis of Nb2O5/Nb2CTx

60 mg layered Nb2CTx was added in 150 mL deionized water and stirred for 1 h to form suspension. The suspension was then transferred into an autoclave for hydrothermal oxidation at 200 ◦C for 12 h, 18 h and 30 h, respectively. The Nb2O5/Nb2CTx samples were then obtained and denoted as Nb2CTx-12, Nb2CTx-18 and Nb2CTx-30, respectively.

For comparison, the pure Nb2O5 was prepared by calcination of Nb2CTx in air at 800 ◦C for 2 h and denoted as C–Nb2O5.

  - Characterization

Morphologies of   the   Nb2CTx-12,   Nb2CTx-18,   Nb2CTx-30   and

C–Nb2O5 were observed by a field emission scanning electron micro- scopy (SEM) (JSM-5900LV) and transmittance electron microscopy (TEM) (Tecnai G-F20). XRD patterns were recorded on an X-ray diffractometer under Cu Kα radiation (λ 1.54 Å) at 40 kV and 40 mA. X-ray photoelectron spectroscopy (Thermo Scientific Escalab 250Xi) was used to determine chemical composition of Nb2CTx-30. Raman spectra were obtained by Andor SR-500i spectrometer with laser exci- tation at λ = 532 nm. The BET surface areas were obtained by a Micromeritics Gemini VII 2390 system. UV–vis diffuse reflectance spectra (DRS) in the range of 200-800 nm were carried out on a UV–Vis spectrophotometer (UV-2700, Shimadzu, Japan). Fluorescence spec- trometer (FLS1000, Edinburgh) was used to measure photo- luminescence (PL) spectra at an excitation source of 325 nm. Electron paramagnetic resonance (EPR, Bruker EMXplus) spectrometer was used to detect the active species and the DMPO was used as capture agents for

=

and •OH.

  - Photoelectrochemical properties  measurement

Photoelectrochemical measurements were conducted in a standard three-electrode system using an electrochemical workstation (CHI 660 E, China). ITO with coated samples, platinum plate and Ag/AgCl elec- trode were used as working electrode, counter electrode and reference electrode, respectively. The preparation of the working electrode was listed as follows. 4 mg of photocatalysts were added in the mixed 500 μL

solution of Nafion/ethanol (1:4) and sonication for 1 h. The photo- catalysis dispersion (5 μL) was coated on the ITO glass (1 cm2). 0.2 mol L—1 Na2SO4 was used as the electrolyte for the electrochemical imped-

ance spectroscopy (EIS), Mott-Schottky (M-S) curve and photocurrent measurement.

  - Photocatalytic degradation measurement

The photocatalytic degradation properties of Nb2O5/Nb2CTx for RhB dye and TC-HCl were evaluated in a glass vessel under visible-light irradiation using a 500 W Xe lamp (GXZ500, Shanghai, China). 25 mg

of the photocatalyst was placed into 25 mL solution of pollutant (10 mg

L—1). The suspension was magnetically stirred in the dark for 30 min to arrive at the adsorption-desorption equilibrium. For the photocatalytic degradation tests, 5 mL solution was taken out every 10 min and sepa- rated by filtration. The residual concentrations of RhB and TC-HCl in solution was tested using a 4802 double beam UV–vis spectrophotom- eter according to their absorbance at 550 nm and 356 nm, respectively.

Fig. 1. Illustration of preparation of rod-like Nb2O5/Nb2CTx composites.

The stability and reusability of the photocatalyst were evaluated by photodegrading RhB for five cycles. For recycling test, the catalysts were rinsed with deionized water and ethanol for several times and dried under vacuum at 60 ◦C before each test. In order to evaluate the main active species in the photocatalytic reaction, t-butanol, benzoquinone

(BQ) and EDTA-2Na were selected as trapping reagent of hydroxyl radicals (•OH), superoxide radical (•OH2—) and holes (h+), respectively.

The concentrations of trapping reagent are both 1 mmol/L, and the trapping experimental processes are similar to the photocatalytic ac- tivity test.

# Results and discussion

≈

X-ray diffraction (XRD) patterns of the Nb2AlC and Nb2CTx are shown in Fig. 2a. Compared with the (002) peak at 12.8◦ of Nb2AlC, the newly emerged low-angle (002) peak of Nb2CTx is typical for MXene (Lin et al., 2017a). In addition, XRD pattern of Nb2CTx reveals disap- pearance of the most intense peaks of Nb2AlC at 2θ 39◦, which implies thoroughly removal of interlayer Al (Mashtalir et al., 2015). The (002) peak of Nb2CTx significantly broadens and shifts toward a lower 2θ angle of 9.3◦, suggesting that the layered Nb2CTx MXene is formed. Fig. 2b shows XRD patterns of Nb2CTx after hydrothermal oxidation. Charac- teristic peaks at 22.5◦, 28.2◦, 36.6◦, 46.1◦, 50.1◦, 54.8◦ and 55.7◦ correspond to (001), (100), (101), (002), (110), (102) and (111) planes of the pseudohexagonal phase of Nb2O5, respectively (Yang et al., 2017; Zhao et al., 2012). As the hydrothermal time prolongs, the intensity of diffraction peak of Nb2O5 increases, revealing that the crystallite sizes of Nb2O5 increase. Enhancement of the relative peak intensity of the (001) peak illustrates a significantly preferred orientation of the (001) crystal face in the Nb2O5 materials (Chen et al., 2017). The diffraction peaks of

Nb2CTx cannot be observed in the XRD patterns of Nb2CTx-12, Nb2CTx-18 and Nb2CTx-30, indicating that the surface of the Nb2CTx is completely covered by Nb2O5. The characteristic peaks of pseudohex- agonal phase Nb2O5 and orthorhombic phase Nb2O5 are observed in XRD pattern of C–Nb2O5, indicating the presence of mixed phases in C–Nb2O5. The catalytic activity of pseudohexagonal phase Nb2O5 is higher than that of orthorhombic phase Nb2O5, indicating that the cat- alytic activity of Nb2O5 depends on its crystalline phases (Murayama

et al., 2014). In addition, the Raman spectra of Nb2CTx-30 and C–Nb2O5 are presented in Fig. S1. The characteristic peaks at 239 cm—1 and 709 cm—1 of Nb2CTx-30 and C–Nb2O5 are assigned to Nb2O5. Peaks at 529, 903 and 1558 cm—1 corresponding to the characteristics of Nb2CTx can

be obviously observed in Raman spectrum of Nb2CTx-30. The results reveal that the Nb2CTx is partially oxidized during the hydrothermal treatment and Nb2O5 is formed on the Nb2CTx.

SEM images of the Nb2AlC, Nb2CTx, Nb2O5/Nb2CTx composites and

C–Nb2O5 are shown in Fig. 3 and Fig. S2. Compared with the bulk Nb2AlC (Fig. S2a), the Nb2CTx (Fig. S2b) is composed of numerous stacked layers. Fig. 3a–c show the morphologies of Nb2O5/Nb2CTx composites. The Nb2O5 nanorods are grown on the surface of the Nb2CTx layers after hydrothermal oxidation for 12 h as shown in Fig. 3a. The formation of Nb2O5 nanorods can be explained by the fact that Nb2O5 are firstly nucleated on the external or interior Nb2CTx layers during hydrothermal treatment and the F group on the surface of Nb2CTx can be regarded as directing reagent (Zhang et al., 2016b). The number of high energy (001) facets is increased during the continuous crystal growth due to the lower energy of (101) planes adsorbing F group. Accordingly, Nb2O5 nanorods with abundant (001) facets are formed (Dong et al., 2017; Li et al., 2019b; Zhou et al., 2013). The amount of Nb2O5 nanorods increase (Fig. 3b and c) with the rise of the time of hydrothermal oxidation because prolonged oxidation time is beneficial to growth of Nb2O5 along the rod orientation. However, the Nb2O5 particles obtained from Nb2CTx by calcination (C–Nb2O5) are agglomerated into a whole bulk as shown in Fig. 3d. Fig. 3e shows SEM of Nb2CTx-30 sample and corresponding element mapping of Nb, O and C. The distribution of O and Nb elements is homogeneous, indicating that Nb2O5 nanorods are grown uniformly on the surface of the Nb2O5/Nb2CTx composite. A small amount of C element is distributed on the surface of the Nb2CTx-30, indicating Nb2CTx is completely covered with Nb2O5 nanorods. In addition, abundant C elements on the edge come from the background.

TEM images of Nb2O5/Nb2CTx composite (Nb2CTx-30) are shown in

Fig. 3f–h and the rod-like Nb2O5 can be obviously observed. The red circle in Fig. 3f shows the interface of Nb2O5 and Nb2CTx, which indicate the successfully growth of Nb2O5 nanorods on the Nb2CTx. The HRTEM image of Nb2O5/Nb2CTx sample (Fig. 3g) shows the crystalline structure with a lattice spacing of 0.394 nm, which match well with the (001) plane of Nb2O5. The (001) plane exposes a mass of active sites, which is conductive to improving the photocatalytic activity (Jiang et al., 2018). In addition, the interplanar spacing of 0.214 nm corresponds to the

(421) plane of Nb2CTx as shown in Fig. 3g and h (Jin et al., 2019). XPS spectra of Nb2CTx, Nb2CTx-30 and C–Nb2O5 are illustrated in

Fig. 4. The Nb 3 d is fitted with three doublets (Nb 3d5/2-Nb 3d3/2) (Fig. 4a). The binding energies peaks at 207.1 (Nb 3d5/2) and 209.9 eV (Nb 3d3/2) in the XPS spectrum of Nb 3 d component are attributed to the strong Nb spin-orbital doublet, which is consistent with the binding energies of Nb2O5 (Liu et al., 2018). The Nb2O5 exist in Nb2CTx because Nb2CTx is slowly oxidized in air to form ultrasmall clusters on the sur- face (Liu et al., 2018). Several weak peaks in the XPS spectrum of Nb2CTx sample are assigned to Nb(4+)-O, Nb(3+)-O and Nb(I, II)–C bonds. The XPS spectrum of Nb2CTx-30 is only fitted with one doublets peak, which corresponds to the binding energies of Nb2O5. Peaks of

Fig. 2. XRD patterns of (a) Nb2AlC, Nb2CTx and (b) Nb2CTx-12, Nb2CTx-18, Nb2CTx-30 and C–Nb2O5.

Fig. 3. SEM images of (a)–(c) Nb2CTx-12, Nb2CTx-18, Nb2CTx-30 and (d) C–Nb2O5; (e)SEM image of Nb2CTx-30 and corresponding elemental mapping images of Nb, O and C; (f)–(h) TEM image and HRTEM image of Nb2CTx-30.

Fig. 4. High-resolution XPS peak of (a) Nb 3 d, (b) C1s, and (c) O 1s peaks in Nb2CTx, Nb2CTx-30 and C–Nb2O5.

Nb2CTx are not observed in the Nb2CTx-30 spectrum, which reveals that the surface of Nb2CTx-30 is completely covered with Nb2O5. The C 1s spectrum of Nb2CTx is fitted by four components located at 281.4, 284.7,

286.2 and 288.0 eV, corresponding to Nb–C, C–C, CHx and O–C–O

bonds, respectively (Hu et al., 2019) (Fig. 4b and Table S1). The O 1s region of Nb2CTx at 530.4, 530.8, 532.0 and 533.3 eV correspond to Nb2O5, C–Nb–O, Nb–OH and H2Oads(Ⅳ), respectively (Fig. 4c). How- ever, Nb–OH bonds cannot be found in Nb2CTx-30 and C–Nb2O5 because the OH groups on the surface disappear after oxidation of Nb2CTx. In addition, the enhanced intensity of C–Nb–O bond in Nb2CTx-30 suggests the increased interaction at the interface of Nb2O5–Nb2CTx.

In order to evaluate the surface areas of Nb2CTx-30 and C–Nb2O5, the nitrogen adsorption/desorption isotherms of Nb2CTx-30 and C–Nb2O5

are illustrated in Fig. 5a. The specific surface area of Nb2CTx-30 and C–Nb2O5 are calculated to be 14.075 m2g-1 and 3.967 m2g-1, respec- tively. The pore-diameter distribution curves are shown in Fig. 5b. It can

be observed that the pore diameter of C–Nb2O5 exceeds 100 nm, while the size of Nb2CTx-30 is about 10 nm. Compared with the bulk C–Nb2O5, specific surface area of Nb2CTx-30 is higher than that of C–Nb2O5 because plenty of Nb2O5 nanorods are grown on the surface of Nb2CTx- 30, which provides abundant small pores. The improved specific surface area of Nb2CTx-30 exposes more activity sites and small pore diameter facilitates the absorption and reactant of active species on their surface, contributing to improve photocatalytic activity.

The optical absorption properties of the Nb2CTx, Nb2O5/Nb2CTx composites and C–Nb2O5 were measured by UV–vis DRS. The Nb2O5/ Nb2CTx composites exhibit a strong absorption in the visible-light region as shown in Fig. 6a due to the full-spectrum absorption of Nb2CTx (Li et al., 2019b). It can be observed that the Nb2O5/Nb2CTx composites possess absorption in the visible-light region, which contributes to enhance the photoactivity in the visible-light region. In addition, the absorption intensity of Nb2CTx-12, Nb2CTx-18 and Nb2CTx-30 decrease successively in the wide visible range due to the extension of hydro- thermal oxidization time, which cause that more Nb2CTx is conversed to Nb2O5. The C–Nb2O5 exhibits significant absorption in the UV region, but no light absorption in the visible-light region. The band-gap energy of the Nb2O5/Nb2CTx composites and C–Nb2O5 were determined by using the Tauc plots method as formula (1).

1/n

eV, 3.13 eV and 3.14 eV, respectively. The difference in band gap be- tween Nb2O5/Nb2CTx composites and C–Nb2O5 is resulted from their different crystalline phase, moreover, the photocatalytic activity of orthorhombic phase Nb2O5 (C–Nb2O5) is conspicuously lower than that of pseudohexagonal phase (Nb2O5/Nb2CTx) as previous literature re- ported (Qi et al., 2013). The corresponding absorption edges (λg, λg = 1240/Eg) for C–Nb2O5, Nb2CTx-12, Nb2CTx-18 and Nb2CTx-30 are 423 nm, 408 nm, 396 nm and 395 nm, respectively, which are calculated according to the band gap energy. Although all the Nb2CTx/Nb2O5 samples possess narrower absorption edge than C–Nb2O5, the presence of Nb2CTx of Nb2CTx/Nb2O5 samples can enhance the visible light ab- sorption ability.

The photoelectrochemical performance of all the as-prepared sam- ples was investigated by transient photocurrent responses and electro- chemical impedance spectroscopy (EIS). The photocurrent-time (I-t) curves of the samples with repeated on-off cycles of visible light irra- diation are shown in Fig. 6c. Generally, stronger photocurrent intensity indicates more effective separation and migration of photoinduced charge carriers (Li et al., 2019b). The Nb2CTx-30 composite exhibits strongest photocurrent response, which implies that Nb2CTx-30 com- posite exhibits higher separation and transfer efficiency of photo- generated charge carriers. However, the Nb2CTx shows high current density but no photocurrent response characteristics, indicating no photocatalytic activity. The transfer and recombination abilities of photogenerated electron-hole pairs of the photocatalysts is further estimated by electrochemical impedance spectroscopy (EIS) (Liu et al., 2019). The smaller arc radius on the EIS Nyquist plot signifies smaller charge transfer resistance on the working electrode surface and higher electron-hole pair separation efficiency. Compared with Nb2CTx-12, Nb2CTx-18, Nb2CTx-18 and C–Nb2O5, the EIS curve of Nb2CTx shows negligible arc radius due to the intrinsic conductivity of Nb2CTx (Fig. 6d). The arc radius of Nb2CTx-30 is smaller than that of Nb2CTx-12 Nb2CTx-18 and C–Nb2O5, indicating Nb2CTx-30 has higher photoin- duced electrons transfer efficiency. In addition, the photoluminescence

(PL) spectra of Nb2CTx, C–Nb2O5 Nb2CTx-12, Nb2CTx-18 and Nb2CTx-30

samples are shown in Fig. S3. It is obvious that the PL emission intensity of C–Nb2O5 is significantly higher than those of Nb2CTx/Nb2O5 com- posites, suggesting that the formed heterojunction interface between

Nb2O5 to Nb2CTx can effectively inhibit the charge recombination. The

(αhv)   = A(hv — Eg)	(1)

Nb2CTx possess no response characteristic in visible light range, thus the

where α, h, v, A and Eg are the absorption coefficient, Planck constant, light frequency, material-dependent constant and the band gap of semiconductor, respectively. “n” represents the transition of semi-

=

conductor having value of n  2 for indirect semiconductor (Nb2O5) (da Silva et al., 2017). The [αhv]1/2 vs. hv plots (Fig. 6b) show the band gaps of C–Nb2O5, Nb2CTx-12, Nb2CTx-18 and Nb2CTx-30 are 2.93 eV, 3.04

generated intensity of PL peak is weak. The results of photocurrent-time curves, electrochemical impedance spectroscopy and photo- luminescence spectra indicate that Nb2CTx-30 exhibits superior photoactivity.

Fig. 7 shows the photocatalytic degradation activities of Nb2CTx, Nb2O5/Nb2CTx composites and C–Nb2O5 for RhB. The absorption of RhB in the presence of photocatalysts reach adsorption/desorption

Fig. 5. (a) Nitrogen adsorption/desorption isotherms and (b) pore diameter distribution of Nb2CTx-30 and C–Nb2O5.

Fig. 6. (a) UV–vis diffuse reflection spectra, (b) plots of (αhv)1/2 versus photon energy, (c) the transient photocurrent responses and (d) electrochemical impedance spectroscopy of Nb2CTx, Nb2CTx-12, Nb2CTx-18, Nb2CTx-30 and C–Nb2O5.

equilibrium in the dark for 30 min. The concentration of RhB decreases to 15.3% in the presence of Nb2CTx due to the slightly adsorption of Nb2CTx as shown in Fig. 7a. The photocatalytic degradation efficiency of C–Nb2O5 is 24.9% because of the low photoactivity of C–Nb2O5 under visible light irradiation. The degradations efficiencies of RhB in the presence of Nb2CTx-12, Nb2CTx-18 and Nb2CTx-30 are 26.9%, 77.5% and 98.5%, respectively (Fig. 7b). The active site of the Nb2O5/Nb2CTx composites is obviously improved for the prolongation of hydrothermal treatment time due to the increase of content of Nb2O5 on the surface of the Nb2CTx, thereby enhancing the photocatalytic degradation effi- ciency. Especially, the photocatalytic degradation efficiency of Nb2CTx- 30 is superior to that of C–Nb2O5 because of the formation of a heter- ojunction between the Nb2O5 and Nb2CTx, resulting in rapid transfer and separation of photogenerated carriers. In addition, the Nb2O5 nanorods on the surface of Nb2CTx, possesses a high specific surface area and exposes more active sites which contributes to the adsorption and degradation of RhB. The reaction kinetics of RhB degradation in the presence of Nb2CTx, C–Nb2O5 and Nb2O5/Nb2CTx composites are illus- trated in Fig. 7c and d. The rate constant (k) of photocatalytic degra-

dation of RhB in the presence of Nb2CTx, Nb2CTx-12, Nb2CTx-18, Nb2CTx-30 and C–Nb2O5 are 0.00099 min—1, 0.0012 min—1, 0.011

min—1, 0.035 min—1 and 0.002 min—1, respectively, suggesting that the Nb2O5/Nb2CTx composites exhibit excellent photocatalytic activity.

The effect of pH in pollutants solution during photocatalytic degra- dation and stability of photocatalysts is an important factor for photo- catalysts in practical application. Fig. 8a shows the influence of pH on the photocatalytic degradation of RhB in the presence of Nb2CTx-30. The photocatalytic degradation efficiencies are 97.7%, 91.4%, 91.7%, 70.5% and 18.1% at pH from 3 to 11, respectively. The result reveals that the

RhB degradation efficiency of Nb2CTx-30 is higher in acidic solution. The isoelectric point of Nb2O5 is 2.8 as previous literature reported (Chandiran et al., 2014), thus negative charged Nb2CTx-30 can adsorb more RhB with diethylamine groups (since its pKa is 3.1) in strong acidic solution (Lops et al., 2019). However, the adsorption of RhB containing carboxyl groups can be inhibited due to the electrostatic repulsion in weakly acidic and alkaline solutions, which results in the decrease of photocatalytic efficiency. The reusability and stability of Nb2CTx-30 photocatalyst for degradation of RhB for five cycles under visible light irradiation are presented in Fig. 8b. The degradation ratio of Nb2CTx-30 for RhB is still 87.6% after five cycles. Compared with the first cycle, the decrease of degradation ratio is resulted from the generated interme- diate products absorbed on the surface of photocatalysts and blocked some active sites (Yuan et al., 2020). To further evaluate the stability of the materials during the recycling progress, the XRD patterns of fresh Nb2CTx-30 and recycled samples are shown in Fig. S4. The position and intensity of the characteristic peaks suggest that the phase structure of photocatalyst is maintained. Overall, the Nb2CTx-30 photocatalyst pos- sesses a good reusability and photocatalytic stability and show great potential for practical application.

The photocatalytic degradation activities of Nb2CTx, Nb2O5/Nb2CTx composites and C–Nb2O5 for tetracycline hydrochloride (TC-HCl) are illustrated in Fig. 9. Photocatalytic degradation efficiency of TC-HCl in the presence of Nb2CTx and C–Nb2O5 after visible light irradiation for 180 min is only 23.6% and 28.5%, respectively. However, the photo- catalytic degradation efficiency of TC-HCl by Nb2CTx-12, Nb2CTx-18 and Nb2CTx-30 are 72.2%, 74.2% and 91.2%, respectively. Photo- catalytic activity of Nb2O5/Nb2CTx composites for TC-HCl is superior to those of Nb2CTx and C–Nb2O5. In addition, the degradation rate of

Fig. 7. (a) The photocatalytic degradation process and (b) photocatalytic degradation efficiency of RhB in the presence of Nb2CTx, Nb2CTx-12, Nb2CTx-18, Nb2CTx- 30 and C–Nb2O5 under visible light irradiation, (c) the corresponding first-order kinetic plots, (d) the rate constant of RhB degradation.

Fig. 8. (a) The photocatalytic degradation of RhB at various pH values from 3 to 11 and (b) five photocatalytic degradation cycles of RhB in the presence of Nb2CTx- 30 under visible light irradiation.

Nb2CTx-30 sample is 13.5 times and 6.8 times as high as Nb2CTx and C–Nb2O5, respectively (Fig. 9b). The effect of pH on degradation of TC- HCl are shown in Fig. 9c. The degradation performance of Nb2CTx-30 on TC-HCl in different pH values was further studied. It is obvious that the photocatalytic degradation efficiency become lower at higher pH value (Fig. 9c). The phenomenon can be explained by the fact that the negative charge on the surface of the tetracycline increases with the rise of pH, resulting in an increase in the electrostatic repulsion with the catalyst and further affecting the photocatalytic efficiency (Zhang et al., 2020).

Five-cycle experiments for TC-HCl degradation were conducted to test the durability of the Nb2CTx-30 composite. The TC-HCl photocatalytic degradation efficiency of the Nb2CTx-30 composite decreases by 5.6% after 5 recycling tests as shown in Fig. 9d, demonstrating the outstanding stability of Nb2CTx-30 composite. Compared with other Nb2O5-based photocatalysts (Fig. S5), Nb2CTx-30 possesses superior degradation efficiency for RhB and TC-HCl. The result indicates that Nb2O5/Nb2CTx composite materials exhibit enhanced visible-light-response photoactivity.

Fig. 9. (a) The photocatalytic degradation of TC-HCl and (b) corresponding.

first-order kinetic plots in the presence of Nb2CTx, Nb2CTx-12, Nb2CTx-18, Nb2CTx-30 and C–Nb2O5; (c) The photocatalytic degrada- tion of TC-HCl at various pH values from 3 to 11 and (d) five photo- catalytic degradation cycles of TC-HCl in the presence of Nb2CTx-30 under visible light irradiation.

In order to reveal the photocatalytic mechanism of rod-like Nb2O5/ Nb2CTx composites, free radicals trapping experiments were performed (Fig. 10). The effects of reactive oxygen species (ROS) of superoxide

radical  anions  (•OH2—),  hydroxyl  radicals  (•OH)  and  hole  (h+)  were

investigated by introducing benzoquinone (BQ), t-butanol and EDTA- 2Na as the scavengers, respectively (da Silva et al., 2017). The photo- catalytic degradation rate of RhB is only 35.1% when the EDTA-2Na is added, which is far lower than degradation rate (98.5%) without scav-

enger. The obvious inhibiting effect indicates that the h+ is main reac-

tive species in the photocatalysis process. The degradation rate of RhB is 44.9% and photocatalytic degradation process is inhibited significantly when benzoquinone (BQ) is used as •OH—2  scavenger. The result suggests

that the •OH—2  also play the important role in the photocatalytic process.

The photocatalytic degradation rate of RhB decreases from to 98.5%– 78.2% when the t-butanol is added, which indicates that the •OH is not the main reactive species.

EPR measurement is performed to further evaluate the active species in Nb2CTx-30 photocatalyst. No obvious signals of DMPO-•OH—2   adduct

and DMPO-•OH adduct are detected in the Nb2CTx-30 photocatalyst under dark condition as shown in Fig. 10b and c. However, four signals with the relative intensity ratio of 1:1:1:1 for is obviously detected under visible light irradiation for 3 min (Fig. 10b). Four characteristic peaks with relative intensity ratio of 1:2:2:1 corresponding to •OH are

observed under visible light irradiation for 3 min as shown in Fig. 10c. The  EPR  results  confirm  •OH—2    and  •OH  are  active  species  for  the

photocatalytic degradation of organic pollutants.

—	=

In order to understand the photocatalytic mechanism, the electronic structure of Nb2CTx-30 composite was analyzed. Mott-Schottky (MS) curve (Fig. S6) shows the conduction band (CB) potential of Nb2CTx-30. It can be found that the MS curve possesses a positive slope, suggesting that Nb2CTx-30 is a typical n-type semiconductor (Cui et al., 2015). The flat band potential obtained from the intercept of the tangent of the MS curves on the x-axis is 0.77 V (vs Ag/AgCl, pH 7). Generally, the CB potential of n-type semiconductor is very close to the flat band potential. The relationship of normal hydrogen electrode potential (NHE) and Ag/AgCl electrode potential is shown in formula (2) (Liu et al., 2020).

E (NHE) = E (Ag/AgCl) — Eθ + 0.059 pH	(2)

where Eθ (Ag/AgCl, at pH = 7) = 0.197 V. The CB potential of Nb2CTx- 30 is determined as – 0.554 V (vs NHE, pH = 7) according to formula (2).

The valence band (VB) potential of Nb2CTx-30 can be calculated according to the formula (3).

EVB= ECB+Eg	(3)

where Eg is the band gap of the semiconductor. The band gap is 3.14 eV for Nb2CTx-30 based on the curve of (αhv)1/2 versus photon energy plotted (Fig. 6b). Therefore, the VB potential of Nb2CTx-30 is 2.586 V.

A possible photocatalytic mechanism of rod-like Nb2O5/Nb2CTx composites for the degradation reaction is proposed (Fig. 11). The electrons are excited into CB of Nb2O5 nanorods and produce electron- hole pairs under visible irradiation. Most of the photoinduced elec- trons are then transferred from the CB of Nb2O5 to Nb2CTx due to the low Fermi level and the electrical conductivity of Nb2CTx. A Schottky barrier may be then established through the interface of Nb2O5 and Nb2CTx

Fig. 10. (a) Tripping experiment of active species for the photocatalytic degradation of RhB over Nb2CTx-30 in the presence of different scavengers, (b) and (c) EPR spectra of Nb2CTx-30 for	and •OH, respectively.

Fig. 11. Possible mechanism for separation and transfer of photogenerated charges of the Nb2O5/Nb2CTx hybrids in the photocatalytic process.

because of the more negative Fermi level Nb2CTx than the (CB) of Nb2O5 (Liu et al., 2018). The Schottky barrier at the interface between Nb2O5 and Nb2CTx could effectively inhibit the electrons from flowing back to Nb2O5, which contribute to separate the photogenerated electrons and

hole. The remainder electrons on the CB of Nb2O5 can reduce O2 to •OH—2

because the CB potential of Nb2O5 is more negative than the reduction

potential  of  O2/•OH2—  (—0.33  V  vs  NHE)  (Yan  et  al., 2019).  The  holes located on the VB can directly react with pollutants and also oxidize H2O to •OH because VB potential of Nb2O5 is more positive than oxidization potential of OH/•OH (2.38 V vs NHE) (Gao et al., 2021; Wang et al., 2020). In the system of rod-like Nb2O5/Nb2CTx composites, the Nb2CTx serves as trap of electrons to inhibit the recombination of electron-hole

pairs. In addition, the holes and generated •OH and •OH2— radicals can continuously decompose the pollutants.

# Conclusions

Rod-like Nb O /Nb CT composites were prepared by a facile hy-

performance sodium/potassium ion batteries with enhanced capacities. ACS Nano 11, 4792–4800.

Du, Y.C., Zhang, S.H., Wang, J.S., Wu, J.S., Dai, H.X., 2018. Nb2O5 nanowires in-situ grown on carbon fiber: a high-efficiency material for the photocatalytic reduction of Cr(VI). J. Environ. Sci. 66, 358–367.

Gao, X., Niu, J., Wang, Y., Ji, Y.F., Zhang, Y.L., 2021. Solar photocatalytic abatement of tetracycline over phosphate oxoanion decorated Bi2WO6/polyimide composites.

2   5	2      x	J. Hazard Mater. 403, 123860.

drothermal oxidation method. The rod-like structure exhibits larger specific surface area, which leads to more exposed active sites under visible light irradiation. The prepared Nb2O5/Nb2CTx composites exhibit excellent photocatalytic efficiency for degradation of RhB and TC-HCl than C–Nb2O5. The sample Nb2CTx-30 degrades 98.5% of RhB for 120 min and 91.2% of TC-HCl for 180 min. In addition, the Nb2O5/ Nb2CTx composite shows excellent reusability and stability. The results suggest that rod-like Nb2O5/Nb2CTx can be used as a promising material for the degradation of dyes and antibiotic contaminants.

# Declaration of competing interest

The authors declare that they have no known competing financial interests or personal relationships that could have appeared to influence the work reported in this paper.

# Acknowledgments

This work was financially supported by The National Natural Science Foundation of China and The Civil Aviation Administration of China (NO. U1833118), Sichuan Science and Technology Program (2019YFG0244).

# Appendix A. Supplementary data

Supplementary data to this article can be found online at https://doi. org/10.1016/j.envres.2020.110587.

# Credit author statement

We make a solemn commitment that the research of “Facile hydro- thermally synthesis of rod-like Nb2O5/Nb2CTx composite for visible- light driven photocatalytic degradation of organic pollutants” was been done independently by our team. The data of the manuscript is true and valid. The manuscript has not been submitted to any journal except Environmental Research.

# References

Adhikari, S., Selvaraj, S., Kim, D.-H., 2019. Construction of  heterojunction photoelectrode via atomic layer deposition of Fe2O3 on Bi2WO6 for highly efficient photoelectrochemical sensing and degradation of tetracycline. Appl.  Catal. B Environ. 244, 11–24.

Chandiran, A.K., Nazeeruddin, M.K., Gratzel, M., 2014. The role of insulating oxides in blocking the charge carrier recombination in dye-sensitized solar cells. Adv. Funct. Mater. 24, 1615–1623.

Chen, J., Wang, H., Huang, G.L., Zhang, Z.Q., Han, L.F., Song, W., Li, M.Y., Zhang, Y.H., 2017. Facile synthesis of urchin-like hierarchical Nb2O5 nanospheres with enhanced visible light photocatalytic activity. J. Alloys Compd. 728, 19–28.

Cui, H.L., Zhu, G.L., Xie, Y., Zhao, W., Yang, C.Y., Lin, T.Q., Gu, H., Huang, F.Q., 2015.

Black nanostructured Nb2O5 with improved solar absorption and enhanced photoelectrochemical water splitting. J. Mater. Chem. A. 3, 11830–11837.

da Silva, G.T.S.T., Carvalho, K.T.G., Lopes, O.F., Ribeiro, C., 2017. g-C3N4/Nb2O5 heterostructures tailored by sonochemical synthesis: enhanced photocatalytic performance in oxidation of emerging pollutants driven by visible radiation. Appl. Catal. B Environ. 216, 70–79.

Di, J., Xia, J.J., Ge, Y.P., Li, H.P., Ji, H.Y., Xu, H., Zhang, Q., Li, H.M., Li, M.N., 2015.

Novel visible-light-driven CQDs/Bi2WO6 hybrid materials with enhanced photocatalytic activity toward organic pollutants degradation and mechanism insight. Appl. Catal. B Environ. 168–169, 51–61.

Ding, L., Wei, Y.Y., Wang, Y.J., Chen, H.B., Caro, J., Wang, H.H., 2017. A two- dimensional lamellar membrane: MXene nanosheet stacks. Angew. Chem. Int. Ed. 56, 1825–1829.

Dong, Y.F., Wu, Z.-S., Zheng, S.H., Wang, X.H., Qin, J.Q., Wang, S., Shi, X.Y., Bao, X.H.,

2017. Ti3C2 MXene-derived sodium/potassium titanate nanoribbons for high-

Hong, Y.Z., Li, C.S., Zhang, G.Y., Meng, Y.D., Yin, B.X., Zhao, Y., Shi, W.D., 2016.

Efficient and stable Nb2O5 modified g-C3N4 photocatalyst for removal of antibiotic pollutant. Chem. Eng. J. 299, 74–84.

Hu, Y., Chen, W., Lei, T.Y., Zhou, B., Jiao, Y., Yan, Y.C., Du, X.C., Huang, J.W., Wu, C.Y.,

Wang, X.P., Wang, Y., Chen, B., Xu, J., Wang, C., Xiong, J., 2019. Carbon quantum dots-modified interfacial interactions and ion conductivity for enhanced high current density performance in lithium-sulfur batteries. Adv. Energy Mater. 9, 1802955.

Jiang, Y., Xie, X., Chen, Y., Liu, Y.J., Yang, R., Sui, G.X., 2018. Hierarchically structured cellulose aerogels with interconnected MXene networks and their enhanced microwave absorption properties. J. Mater. Chem. C. 6, 8679–8687.

Jin, Z.Y., Fang, Y.F., Wang, X.X., Xu, G.F., Liu, M.L., Wei, S., Zhou, C.L., Zhang, Y.L.,

Xu, Y.H., 2019. Ultra-efficient electromagnetic wave absorption with ethanol- thermally treated two-dimensional Nb2CTx nanosheets. J. Colloid Interface Sci. 537, 306–315.

Li, B.S., Lai, C., Zeng, G.M., Huang, D.L., Qin, L., Zhang, M.M., Cheng, M., Liu, X.G., Yi, H., Zhou, C.Y., Huang, F.L., Liu, S.Y., Fu, Y.K., 2019a. Black phosphorus, a rising star 2D nanomaterial in the post-graphene era: synthesis, properties, modifications, and photocatalysis applications. Small 15, 1804565.

Li, L.H., Deng, J.X., Yu, R.B., Chen, J., Wang, Z., Xing, X.R., 2013. Niobium pentoxide hollow nanospheres with enhanced visible light photocatalytic activity. J. Mater. Chem. A. 1, 11894–11900.

Li, Y.J., Yin, Z.H., Ji, G.R., Liang, Z.Q., Xue, Y.J., Guo, Y.C., Tian, J., Wang, X.Z., Cui, H.

Z., 2019b. 2D/2D/2D heterojunction of Ti3C2 MXene/MoS2 nanosheets/TiO2 nanosheets with exposed (001) facets toward enhanced photocatalytic hydrogen production activity. Appl. Catal. B Environ. 246, 12–20.

Lin, H., Gao, S.S., Dai, C., Chen, Y., Shi, J.L., 2017a. A two-dimensional biodegradable niobium carbide (MXene) for photothermal tumor eradication in NIR-I and NIR-II biowindows. J. Am. Chem. Soc. 139, 16235–16247.

Lin, L., Wang, H.Y., Xu, P., 2017b. Immobilized TiO2-reduced graphene oxide nanocomposites on optical fibers as high performance photocatalysts for degradation of pharmaceuticals. Chem. Eng. J. 310, 389–398.

Liu, J.J., Xiong, C.B., Jiang, S.J., Wu, X., Song, S.Q., 2019. Efficient evolution of reactive oxygen species over the coordinated π-delocalization g-C3N4 with favorable charge transfer for sustainable pollutant elimination. Appl. Catal. B Environ. 249, 282–291.

Liu, T.Y., Yang, G.J., Wang, W., Wang, C.X., Wang, M., Sun, X.N., Xu, P., Zhang, J.T.,

2020. Preparation of C3N5 nanosheets with enhanced performance in photocatalytic methylene blue (MB) degradation and H2-evolution from water splitting. Environ. Res. 188, 109741.

Liu, Y.X., Luo, R., Li, Y., Qi, J.W., Wang, C.H., Li, J.S., Sun, X.Y., Wang, L.J., 2018.

Sandwich-like Co3O4/MXene composite with enhanced catalytic performance for Bisphenol A degradation. Chem. Eng. J. 347, 731–740.

Lops, C., Ancona, A., Di Cesare, K.,  Dumontel,  B.,  Garino,  N.,  Canavese,  G., Hernandez, S., Cauda, V., 2019. Sonophotocatalytic degradation mechanisms of Rhodamine B dye via radicals generation by micro- and nano-particles of ZnO. Appl. Catal. B Environ. 243, 629–640.

Mashtalir, O., Lukatskaya, M.R., Zhao, M.Q., Barsoum, M.W., Gogotsi, Y., 2015. Amine- assisted delamination of Nb2C MXene for Li-ion energy storage devices. Adv. Mater. 27, 3501–3506.

Murayama, T., Chen, J.L., Hirata, J., Matsumoto, K., Ueda, W., 2014. Hydrothermal synthesis of octahedra-based layered niobium oxide and its catalytic activity as a solid acid. Catal. Sci. Technol. 4, 4250–4257.

Oliveira, L.C.A., Oliveira, H.S., Mayrink, G., Mansur, H.S., Mansur, A.A.P., Moreira, R.L., 2014. One-pot synthesis of CdS@Nb2O5 core-shell nanostructures with enhanced photocatalytic activity. Appl. Catal. B Environ. 152–153, 403–412.

Peng, C., Wang, H.J., Yu, H., Peng, F., 2017. (111) TiO2-x/Ti3C2 : synergy of active facets, interfacial charge transfer and Ti3+ doping for enhance photocatalytic activity.

Mater. Res. Bull. 89, 16–25.

Peng, C., Yang, X.F., Li, Y.H., Yu, H., Wang, H.J., Peng, F., 2016. Hybrids of two- dimensional Ti3C2 and TiO2 exposing {001} facets toward enhanced photocatalytic activity. ACS Appl. Mater. Interfaces 8, 6051–6060.

Qamar, M., Abdalwadoud, M., Ahmed, M.I., Azad, A.M., Merzougui, B., Bukola, S., Yamani, Z.H., Siddiqui, M.N., 2015. Single-Pot synthesis of 〈001〉-Faceted N-doped Nb2O5/reduced graphene oxide nanocomposite for efficient photoelectrochemical water splitting. ACS Appl. Mater. Interfaces 7, 17954–17962.

Qi, S.S., Zuo, R.Z., Liu, Y., Wang, Y., 2013. Synthesis and photocatalytic activity of electrospun niobium oxide nanofibers. Mater. Res. Bull. 48, 1213–1217.

Ran, J.R., Gao, G.P., Li, F.-T., Ma, T.-Y., Du, A.J., Qiao, S.-Z., 2017. Ti3C2 MXene co-

catalyst on metal sulfide photo-absorbers for enhanced visible-light photocatalytic hydrogen production. Nat. Commun. 8, 13907.

=

Ren, K., Ren, C.D., Luo, Y., Xu, Y.J., Yu, J., Tang, W.C., Sun, M.L., 2019. Using van der Waals heterostructures based on two-dimensional blue phosphorus and XC (X     Ge, Si) for water-splitting photocatalysis: a first-principles study. Phys. Chem. Chem. Phys. 21, 9949–9956.

Rimoldi, L., Meroni, D., Cappelletti, G., Ardizzone, S., 2017. Green and low cost tetracycline degradation processes by nanometric and immobilized TiO2 systems. Catal. Today 281, 38–44.

Shahzad, A., Rasool, K., Nawaz, M., Miran, W., Jang, J., Moztahida, M., Mahmoud, K.A., Lee, D.S., 2018. Heterostructural TiO2/Ti3C2Tx (MXene) for photocatalytic degradation of antiepileptic drug carbamazepine. Chem. Eng. J. 349, 748–755.

4+

Su, T.M., Peng, R., Hood, Z.D., Naguib, M., Ivanov, I.N., Keum, J.K., Qin, Z.Z., Guo, Z.H., Wu, Z.L., 2018. One-step synthesis of Nb2O5/C/Nb2C (MXene) composites and their use as photocatalysts for hydrogen evolution. ChemSusChem 11, 688–699.

Wang, C.D., Chen, S.M., Xie, H., Wei, S.Q., Wu, C.Q., Song, L., 2019. Atomic Sn decorated into vanadium carbide MXene interlayers for superior lithium storage. Adv. Energy Mater. 9, 1802977.

Wang, H., Peng, R., Hood, Z.D., Naguib, M., Adhikari, S.P., Wu, Z.L., 2016. Titania composites with 2 D transition metal carbides as photocatalysts for hydrogen production under visible-light irradiation. ChemSusChem 9, 1490–1497.

Wang, H., Wu, Y., Yan, X.Z., Zeng, G.M., Zhou, J., Wang, X., Chew, J.W., 2018. Clay- inspired MXene-based electrochemical devices and photo-electrocatalyst: state-of- the-art progresses and challenges. Adv. Mater. 30, 1704561.

Wang, Y.T., Zhu, C.Z., Zuo, G.C., Guo, Y., Xiao, W., Dai, Y.X., Kong, J.J., Xu, X.M., Zhou, Y.X., Xie, A.M., Sun, C., Xian, Q.M., 2020. 0D/2D Co3O4/TiO2 Z-Scheme

heterojunction for boosted photocatalytic degradation and mechanism investigation. Appl. Catal. B Environ. 278, 119298.

Yan, W., Yan, L., Jing, C.Y., 2019. Impact of doped metals on urea-derived g-C3N4 for photocatalytic degradation of antibiotics: structure, photoactivity and degradation mechanisms. Appl. Catal. B Environ. 244, 475–485.

Yang, H.L., Xu, H.H., Wang, L.B., Zhang, L., Huang, Y.H., Hu, X.L., 2017. Microwave- assisted rapid synthesis of self-assembled T-Nb2O5 nanowires for high-energy hybrid supercapacitors. Chemistry 23, 4203–4209.

Yi, J.J., Li, H.P., Gong, Y.J., She, X.J., Song, Y.H., Xu, Y.G., Deng, J.J., Yuan, S.Q., Xu, H.,

Li, H.M., 2019. Phase and interlayer effect of transition metal dichalcogenide

cocatalyst toward photocatalytic hydrogen evolution: the case of MoSe2. Appl. Catal. B Environ. 243, 330–336.

Yuan, R.R., Qiu, J.L., Yue, C.L., Shen, C., Li, D.W., Zhu, C.Q., Liu, F.Q., Li, A.M., 2020.

Self-assembled hierarchical and bifunctional MIL-88A(Fe)@ZnIn2S4 heterostructure as a reusable sunlight-driven photocatalyst for highly efficient water purification. Chem. Eng. J. 401, 126020.

Zhang, C., Beidaghi, M., Naguib, M., Lukatskaya, M.R., Zhao, M.-Q., Dyatkin, B., Cook, K.

M., Kim, S.J., Eng, B., Xiao, X., Long, D.H., Qiao, W.M., Dunn, B., Gogotsi, Y., 2016a. Synthesis and charge storage properties of hierarchical niobium pentoxide/carbon/ niobium carbide (MXene) hybrid materials. Chem. Mater. 28, 3937–3943.

Zhang, C.J., Kim, S.J., Ghidiu, M., Zhao, M.-Q., Barsoum, M.W., Nicolosi, V., Gogotsi, Y., 2016b. Layered orthorhombic Nb2O5@Nb4C3Tx and TiO2@Ti3C2Tx hierarchical composites for high performance Li-ion batteries. Adv. Funct. Mater. 26, 4143–4151.

Zhang, Q.C., Jiang, L., Wang, J., Zhu, Y.F., Pu, Y.J., Dai, W.D., 2020. Photocatalytic degradation of tetracycline antibiotics using three-dimensional network structure perylene diimide supramolecular organic photocatalyst under visible-light irradiation. Appl. Catal. B Environ. 277, 119122.

Zhang, Y., Zhao, H., Zhao, X.F., Lin, J.N., Li, N., Huo, Z.Y., Yan, Z.F., Zhang, M., Hu, S.,

2018. Narrow-bandgap Nb2O5 nanowires with enclosed pores as high-performance photocatalyst. Sci. China Mater. 62, 203–210.

Zhao, L.J., Wang, K., Wei, W., Wang, L.L., Han, W., 2019. High-performance flexible sensing devices based on polyaniline/MXene nanocomposites. Info 1, 407–416.

Zhao, Y., Eley, C., Hu, J.P., Foord, J.S., Ye, L., He, H.Y., Tsang, S.C.E., 2012. Shape-

dependent acidity and photocatalytic activity of Nb2O5  nanocrystals with  an active TT (001) surface. Angew. Chem. Int. Ed. 51, 3846–3849.

Zhou, W.J., Yin, Z.Y., Du, Y.P., Huang, X., Zeng, Z.Y., Fan, Z.X., Liu, H., Wang, J.Y.,

Zhang, H., 2013. Synthesis of few-layer MoS2 nanosheet-coated TiO2 nanobelt heterostructures for enhanced photocatalytic activities. Small 9, 140–147.